Pella® Lifestyle Series In-Swing Patio Door
Aluminum EnduraClad® Exterior
Detailed Product Description

Frame 
•	Select softwood, immersion treated with Pella’s EnduraGuard® wood protection formula in accordance with WDMA I.S.-4. The EnduraGuard formula includes three active ingredients for protection against the effects of moisture, decay, stains from mold and mildew. Plus, an additional ingredient adds protection against termite damage.
•	Interior exposed surfaces are clear pine, edge-banded or veneered.
•	Exterior surfaces are clad with aluminum at the head and jambs. 
•	Components are assembled with screws, staples and concealed corner locks.
•	Frame depth between 5-7/8" (149 mm) to 8-5/8" (219 mm), for wall depth between 4-9/16" (116 mm) to 7-5/16" (186 mm).
•	Optional factory-applied EnduraClad® exterior trim.
•	Solid extruded aluminum sill with [black] [mill] finish with oak threshold.
Door Panels 
•	Select softwood, immersion treated with Pella’s EnduraGuard® wood protection formula in accordance with WDMA I.S.-4. The EnduraGuard formula includes three active ingredients for protection against the effects of moisture, decay, stains from mold and mildew. Plus, an additional ingredient adds protection against termite damage.
•	Interior exposed surfaces are veneered with clear pine with no visible fastener holes.
•	Exterior surfaces are clad with aluminum.
•	Panel rails and hinge stiles are three-ply construction, randomly finger-jointed blocks laminated with water-resistant glue and pine-veneered on both sides.
•	Panel lock stiles are constructed with LVL core with clear pine edge bands on both sides and veneered on both faces.
•	Corners are urethane-sealed and secured with metal fasteners.
•	Panel thickness is 2-1/16" (52 mm).
Weatherstripping 
•	Dual-durometer extruded polymer along perimeter of door frames and along the bottom of door panels.
Glazing System
•	Quality fully-tempered float glass complying with ASTM C 1048.
•	High altitude glazing available.
•	Dual-Pane Glazing:
•	Silicone-glazed 13/16" [obscure1] dual-seal insulating glass [[Advanced] [SunDefense™] [SunDefense+] [AdvancedComfort] [NaturalSun] [NaturalSun+] Low-E [with argon].
•	Triple-Pane Glazing:
•	Exterior dual-seal insulating glass, silicone-glazed 11/16", [obscure] [[Advanced] [SunDefense™] [SunDefense+] [AdvancedComfort] [NaturalSun] [NaturalSun+] Low-E [with argon]] [[bronze] [gray] [green] Advanced Low-E with argon].
•	Interior hinged clear tempered glass panel set in a [veneered (for stain fishes)] aluminum frame, fitted to door panel with continuous gasket seal.
•	Airspace between insulating glass and hinged glass panel is 1-1/32". 
Exterior 
•	Aluminum clad exteriors shall be finished with EnduraClad® protective finish, in a multi-step, baked-on finish.
•	Finish color:
•	Finish color [Standard [Black] [White] [Brown] [Fossil]] [Feature [Iron Ore] Wolf gray] [Classic White] [Almond] [Portobello] [Putty] [Brick Red] [Hartford Green]].
Interior 
•	[Unfinished, ready for site finishing] [factory primed with one coat acrylic latex] [factory prefinished [White] [Linen White] [Bright White] [stain1]].
Hardware 
•	Hinges are adjustable to help with installation.
•	Doors over 7' 0" frame height have four (4) hinges per panel.
•	Doors 7' 0" and under frame height have three (3) hinges per panel.
•	Mortised and keyed multi-point locking system, center deadbolt and shoot-bolts at head and sill will engage simultaneously.
•	Solid brass handles and keylock with K-keyway cylinder.
•	Key cylinder finish is [Brass] [Stainless Steel] [Matte Black].
•	Hardware finish (Handle, Hinges and Strike) is [baked enamel [White] [Champagne] [Brown] [Matte Black]] [Satin Brass] [Satin Nickel].

Optional Products
Grilles
•	Simulated-Divided-Light [with optional spacer] (Dual-pane glazing)
•	7/8" Grilles permanently bonded to the interior and exterior of glass.
•	Patterns are [Traditional] [Prairie] [Cross] [Top Row] [Custom – Equally Divided].
•	Interior surfaces are [unfinished, ready for site finishing] [factory primed] [pine: factory prefinished [White] [Linen White] [Bright White] [stain1]].
•	Exterior color to match the exterior cladding color.
•	Simulated-Divided-Light with Grilles-Between-the-Glass (Triple-pane glazing)
•	3/4" Grilles permanently bonded to the exterior of glass.
•	Patterns are [Traditional] [Prairie] [Cross] [Top Row] [Custom – Equally Divided].
•	Exterior color to match the exterior cladding color.
•	Insulating glass contains 3/4" contoured aluminum grilles permanently installed between two panes of glass.
•	Interior color is [White] [Ivory] [Tan3] [Brickstone] [Black] [Putty3] [Brown3] [Harvest] [Cordovan].
– or –
•	Grilles-Between-the-Glass2
•	Insulating glass contains 3/4" contoured aluminum grilles permanently installed between two panes of glass.
•	Patterns are [Traditional] [9-Lite Prairie] [Top Row] [Cross] [Custom – Equally Divided].
•	Interior color is [White] [Ivory] [Tan3] [Brickstone3] [Black] [Putty3] [Brown] [Harvest] [Cordovan].
•	Exterior color [matched to the exterior cladding color] [White]4.
Screens
•	Finish matches exterior cladding.
•	Hinged Insect Screens:
•	Compliance:  ASTM D 3656 and the performance requirements of SMA 1201.
•	Screen Cloth:  InView™ Vinyl-coated fiberglass, 18/18 mesh fiberglass screen cloth complying the performance requirements of SMA 1201.
•	Extruded-aluminum frame, hinged to door frame.
•	Complete with necessary hardware.
•	Hardware Color: [Champagne] [Matte Black] [White] [Oil-Rubbed Bronze] [Satin Nickel].
– or –
•	Exterior Sliding Insect Screens:
•	Compliance:  ASTM D 3656 and the performance requirements of SMA 1201.
•	Screen Cloth:  InView™ Vinyl-coated fiberglass, 18/18 mesh fiberglass screen cloth complying the performance requirements of SMA 1201.
•	Extruded-aluminum frame, top hung on 2 adjustable nylon rollers.
•	Complete with necessary hardware.
•	Hardware Color: [White] [Tan] [Brown] [Matte Black].

Integrated Between-the-Glass Window Fashions (Triple-Pane glazing only)1
•	Slimshade® Blinds 
•	15 mm aluminum slat, bottom-up blinds with polyester cord ladder
•	Installed in sash between double glazing and interior hinged glass panel.
•	Operated with cordless operator or motorized with Insynctive® technology. 
– or –
•	Cellular Fabric Shades
•	11/16" width, bottom-up shades with hidden polyester cord, spun bond Polyethylene Terephthalate (PET) cellular fabric.
•	Installed in sash between double glazing and interior hinged glass panel.
•	Operated with cordless operator or motorized with Insynctive® technology.
Sensors
•	Optional factory installed integrated security sensors available in vent units.  

(1)	Contact your local Pella sales representative for current designs and color options.
(2)	Available on units glazed with Low-E insulated glass with argon, and obscure insulated glass.
(3)	Tan, brickstone and putty Interior GBG colors are available only with matching interior and exterior colors.
(4)	Appearance of exterior grille color will vary depending on Low-E coating on glass.