Pella® Reserve - Traditional Awning and Large Awning 
Wood Exterior
Detailed Product Descriptions

Frame
•	Select softwood, immersion treated with Pella’s EnduraGuard® wood protection formula in accordance with WDMA I.S.-4. The EnduraGuard formula includes three active ingredients for protection against the effects of moisture, decay, stains from mold and mildew. Plus, an additional ingredient adds protection against termite damage.
•	Interior exposed surfaces are [clear pine] [mahogany]. 
•	Exterior surfaces are [pine: factory-primed] [mahogany: [factory-primed] [ready-to-stain]].
•	Overall frame depth is 4-3/8" (111 mm) for a wall depth of 4-3/16" (10 mm).
•	Optional factory-applied jamb extensions available between 3-13/16" (97mm) and 9-3/16" (233mm).
Sash
•	Select softwood, immersion treated with Pella’s EnduraGuard® wood protection formula in accordance with WDMA I.S.-4. The EnduraGuard formula includes three active ingredients for protection against the effects of moisture, decay, stains from mold and mildew. Plus, an additional ingredient adds protection against termite damage.
•	Interior exposed surfaces are [clear pine] [mahogany].
•	Exterior Surfaces are [pine: factory-primed] [mahogany [factory-primed] [ready-to-stain]].
•	Corners mortised and tenoned, glued and secured with metal fasteners. 
•	Sash thickness is [1-13/16" (46mm) for 11/16"] [2-1/8" (54mm) for 1"] glazing.
•	Sash exterior profile is putty glaze, interior profile is ogee.
Weatherstripping
•	Dual weatherstripping. 
•	Continuous, flexible santoprene material in dual durometer design with welded corners, compressed between frame and sash for positive seal on all four sides. 
•	Secondary thermoplastic vulcanizate (TPV) leaf-type weatherstrip between edge of sash and frame.
Glazing System1
•	Quality float glass complying with ASTM C 1036.
•	Custom and high altitude [with argon] glazing available.
•	Silicone-glazed 11/16" dual-seal insulating glass [[annealed] [tempered]] [[clear] [[Advanced] [SunDefense™] [SunDefense+] [AdvancedComfort] [NaturalSun] [NaturalSun+] Low-E [with argon]] [[bronze] [gray] [green] Advanced Low-E with argon]].
– or –
•	Silicone-glazed 1” triple-pane, dual-seal insulating glass [[annealed] [tempered]] [[Advanced] [SunDefense™] [NaturalSun] Low-E [with argon]]
Interior
•	[Unfinished, ready for site finishing] [factory primed with one coat acrylic latex] [Pine: Factory prefinished [paint] [stain] 3].
Hardware
•	Roto operator assembly
•	Steel worm gear sash operator with hardened gears.
•	Operator base to be zinc die cast with painted finish. 
•	Operator linkage, hinge slide, and hinge arms are stainless steel. 
•	Exposed fasteners are stainless steel. 
•	Hardware will exceed 1,000 hours salt spray exposure per ASTM B 117. 
•	Hinge slide and hinge arms are stainless steel.
•	All vent units are available with operator located on the [Awning: left or right side as viewed from the exterior] [Large Awning or Impact-Resistant: bottom center of the unit].
•	SureLock® System—A single handle locking system operates positive-acting arms that reach out and pull the sash into a locked position: [Awning: one operating lock installed on units with frame widths 29" and less, two unison operating locks installed on units with frame widths over 29"] [Large Awning: one operating lock installed on units with frame heights 41" and less, two unison operating locks installed on units with frame height over 41"]. 
•	Style of hardware is [Standard integrated fold-away crank and standard lock handle with [baked enamel [Champagne] [White] [Brown] [Matte Black]] [satin brass] [satin nickel] [oil-rubbed bronze] hardware finish] [Antiek fold-away crank and Antiek lock handle with [baked enamel [Champagne] [White] [Brown] [Matte Black]] [Satin Brass] [Satin Nickel] [Oil-rubbed Bronze] [Distressed Bronze] [Distressed Nickel] hardware finish]. 

Optional Products
Grilles
•	Integral Light Technology® grilles
•	Interior grilles are solid [5/8”] [7/8"] [1-1/4"] ogee profile that are solid [pine] [mahogany]. Interior surfaces are [unfinished, ready for site finishing] [factory primed] [pine: factory prefinished [paint] [stain] 3].
•	Exterior grilles are solid [5/8”] [7/8"] [1-1/4"] putty glaze profile] that are [pine] [mahogany]. Exterior surfaces are water repellent, preservative-treated in accordance with WDMA I.S.-4, and are [unfinished, ready for site finishing] [factory primed]. 
•	Patterns are [Traditional] [Prairie] [Top Row] [Cross] [New England] [Victorian] [Diamond].
•	Insulating glass contains non-glare spacer between the panes of glass.
•	Grilles are adhered to both sides of the insulating glass with VHB acrylic adhesive tape and aligned with the non-glare spacer.
– or –
•	Grilles-Between-the-Glass2
•	Insulating glass contains 3/4" contoured aluminum grilles permanently installed between two panes of glass (exterior air-space on triple-pane insulating glass). 
•	Patterns are [Traditional] [Prairie] [Cross] [Top Row] [Custom – Equally Divided].
•	Interior color is [Black] [White] [Brown4] [Fossil] [Harvest] [Cordovan] [Ivory] [Tan4] [Brickstone] [Putty4].
•	Exterior color5 is [standard3].
Screens
•	InView™ Screens
•	Vinyl-coated 18/18 mesh fiberglass screen cloth complying with the performance requirements of SMA 1201, set in aluminum frame fitted to inside of window, supplied complete with all necessary hardware.
•	Screen frame finish is [baked enamel [Champagne] [White] [Brown] [Black]] [Wrapped in wood veneer, factory prefinished stain to match interior finish].
Hardware
•	Optional factory applied limited opening hardware available for vent units in stainless steel; nominal 3" opening.
Sensors
•	Optional factory installed integrated security sensors available in vent units.

(1) Low-E coated insulating glass is argon-filled (except high altitude). All other insulating glass (including high altitude Low-E) is air-filled.
(2) Available in clear or Low-E insulating glass only.
(3) Contact your local Pella sales representative for current designs and color options.
(4) Tan, Brown or Putty Interior GBG colors are available in single-tone (Brown/Brown, Tan/Tan or Putty/Putty). Other interior colors are also available with Tan or Brown exterior.
(5) Appearance of exterior grille color will vary depending on Low-E coating on glass.