Pella® Reserve – Traditional Monumental Double-Hung Windows
Wood Exterior
Detailed Product Descriptions

Frame 
•	Select wood, immersion treated with Pella’s EnduraGuard® wood protection formula in accordance with WDMA I.S.-4. The EnduraGuard formula includes three active ingredients for protection against the effects of moisture, decay, stains from mold and mildew. Plus, an additional ingredient adds protection against termite damage.
•	Interior exposed surfaces are [clear pine] [mahogany] curved members may have visible finger joints.
•	Exterior surfaces are [pine] [mahogany]. 
•	Vinyl Jamb liner includes wood inserts.
•	Overall frame depth is 5-5/8" (143mm) for a wall depth of 5-7/16" (138mm).
•	Optional factory applied jamb extensions available from 5-7/16" (138mm) and 7-3/16" (183mm) wall depths.
•	Optional factory installed fold-out installation fins with flexible fin corners.
•	Optional factory-applied pine [1-7/8"] [3-1/2"] brickmould and [1-1/8"] [1-7/8"] subsill.
Sash 
•	Select wood, immersion treated with Pella’s EnduraGuard® wood protection formula in accordance with WDMA I.S.-4. The EnduraGuard formula includes three active ingredients for protection against the effects of moisture, decay, stains from mold and mildew. Plus, an additional ingredient adds protection against termite damage.
•	Interior exposed surfaces are [clear pine, curved members may have visible finger joints] [mahogany (not available if sash weight > 200 lbs.)].
•	Exterior surfaces are [pine] [mahogany]. 
•	Corners mortised and tenoned, glued and secured with metal fasteners. 
•	Sash thickness is 2-1/4" (57mm).
•	Exterior sash profile is putty glaze, interior sash profile ogee.
•	Double-hung upper sash (if sash weight ≤ 92 lbs.) has surface-mounted wash locks for tilt-in cleaning.
•	Double-hung and single-hung lower sash (if sash weight ≤ 92 lbs.) has concealed wash locks in lower check rail for tilt-in cleaning.
Weatherstripping 
•	Santoprene-wrapped foam at head and sill.
•	Full length glass filled polypropylene interlocker with integrated slip-coated thermoplastic elastomer leaf.
•	Secondary nylon bristle rain strip on lower sash at sill.
•	Vinyl-wrapped foam with secondary nylon bristle rain strip inserted into jamb liner to seal against sides of sash.
Glazing System
•	Quality float glass complying with ASTM C 1036.
•	Custom and high altitude glazing available.
•	Silicone-glazed dual-pane 13/16" dual-seal insulating glass [[annealed] [tempered]], [[clear] [[Advanced] [SunDefense™] [SunDefense+] [NaturalSun] [NaturalSun+] [AdvancedComfort] Low-E [with argon]] [[bronze] [gray] [green] Advanced Low-E [with Argon]] [obscure] [Reflective Bronze] [Reflective Gray]
or-
•	Silicone-glazed dual-pane 13/16" dual-seal tempered spandrel glass [Lava Bronze Amber] [Black] [Ford Blue] [Symmetry Bronze] [Symmetry Gray] [Symmetry Green].
-or-
•	Silicone-glazed dual-pane 13/16" dual-seal [[annealed] [tempered]] non-impact laminated glass [[clear] [[Advanced] [SunDefense] Low-E [with Argon]] [[bronze] [gray] [green] Advanced Low-E [with argon]].
– or –
•	Silicone-glazed triple-pane 1-1/16" dual-seal insulating glass (not available if sash weight > 200 lbs.) [[annealed] [tempered]] [[Advanced] [SunDefense™] [NaturalSun] Low-E [with  [argon]] [Obscure [standard] [fern]].
Exterior 
•	[Pine: factory primed with one coat acrylic latex] [Mahogany: [factory primed with one coat acrylic latex] [Unfinished, ready for site finishing]].
Interior 
•	[Unfinished, ready for site finishing] [factory primed with one coat acrylic latex] [pine: factory prefinished [paint] [stain] 1].
Hardware 
•	Galvanized block-and-tackle balances are attached to self-locking balance shoes connected to the sashes using zinc die cast terminals concealed within the frame.
-or-
•	Class 5 hybrid balance attached to [locking] [non-locking] balance shoes connected to the sashes using zinc die cast terminals and concealed within the frame.
-or-
•	Galvanized block-and-tackle balances combined with a Class 5 hybrid balance attached to non-locking balance shoes connected to the sashes using zinc die cast terminals and concealed within the frame.
•	All balances comply with AAMA 902 specification
•	Sash lock is [standard (cam-action)] [historic spoon-style] [air-conditioner lock] [simulated lock (Single-piece lock ties upper and lower sash together. When removed, lower sash becomes operable)]. Two sash locks on units with frame width 37" and greater.
•	Hardware finish is [baked enamel [Champagne] [White] [Brown] [Matte Black]] [Satin Brass] [Satin Nickel] [Oil-rubbed Bronze] [Distressed Bronze] [Distressed Nickel]. 
Optional Products
Grilles
•	Integral Light Technology® grilles
•	Interior grilles are [5/8"] [7/8"] [1-1/4"] [2"] ogee profile that are solid [pine] [mahogany]. Interior surfaces are [unfinished, ready for site finishing] [factory primed] [pine: factory prefinished [paint] [stain] 1].
•	Exterior grilles are solid [5/8"] [7/8"] [1-1/4"] [2"] putty glaze profile that are [pine] [mahogany]. Exterior surfaces are water repellent, preservative-treated in accordance with WDMA I.S.-4, and are [unfinished, ready for site finishing] [factory primed]. 
•	Patterns are [Traditional] [Prairie] [Top Row] [Cross] [New England] [Victorian].
•	Insulating glass contains non-glare spacer between the panes of glass.
•	Grilles are adhered to both sides of the insulating glass with VHB acrylic adhesive tape and aligned with the non-glare spacer.
– or –
•	Grilles-Between-the-Glass2
•	Insulating glass contains 3/4" contoured aluminum grilles permanently installed between two panes of glass (exterior air-space on triple-pane insulating glass).
•	Patterns are [Traditional] [Prairie] [Cross] [Top Row]
•	Interior color is [Black] [White] [Brown3] [Fossil] [Harvest] [Cordovan] [Ivory] [Tan3] [Brickstone] [Putty3].
•	Exterior color4 is [standard1].
Screens
•	InView™ Screens
•	[Full-screen (not available on units > 120" tall)] [half-screen] black Vinyl-coated 18/18 mesh fiberglass screen cloth complying with the performance requirements of SMA 1201, set in aluminum frame fitted to outside of window, supplied complete with all necessary hardware.
•	Full screen spreader bar placed on units > 37" width or > 65" height.
•	Screen frame finish is [standard screen: baked enamel] [premium extruded: [baked enamel] [anodized]], color to match window cladding.
Hardware
•	Optional sash lift furnished for field installation. Finish matches lock hardware. Two lifts on units having frame width 37" or greater.
•	Optional factory applied limited opening device available for venting units; nominal 3-3/4" opening. Limiting device concealed from view.
•	Optional factory applied window opening control device for venting units. Sash mounted device allows window to open less than 4” with normal operation, with a release mechanism that allows the sash to open completely. Finish matches lock hardware. Complies with ASTM F2090-10.
•	Optional [head, sill, stool locks].
Sensors
•	Optional factory installed integrated security sensors available in vent units.

(1) Contact your local Pella sales representative for current color options.
(2) Available in clear or Low-E Insulating Glass only.
(3) Tan, Brown and Putty Interior GBG colors are available in single-tone (Brown/Brown, Tan/Tan or Putty/Putty). Other interior colors are also available with Tan or Brown exterior.
(4) Appearance of exterior grille color will vary depending on Low-E coating on glass.